1 of 2

[image: image1.png]NYATI PAINTS

PO Box 34 252 Greyling Crescent VAT: 4610240287 Tel: (012) 541 3634
Montana Park Rosslyn East CK: 2007/028054/23 (012) 541 0627
0159 Pretoria nyati@nyatipaints.co.za Fax: (012) 541 0031

Mansfacturens of Quality Paists




 SEQ CHAPTER \h \r 1
PRODUCT DATA:


RUST INHIBITIVE, SELF ETCH

(CODE 4106)


SEMI – GLOSS, EMULSION PAINT
DESCRIPTION
A pure acrylic, anti-corrosive, water based primer, with top coat inheritance properties.  Low sheen appearance.  For use on mild steel and galvanized surfaces.  Quick – drying, highly resistant to chemical attack and ultra violet light.
BENEFITS
Easily stored.
Nontoxic – Water borne.
Non-flammable.
One pack multi function product.

Easy application.

Available in various colours.

LIMITATIONS AND PRECAUTIONS
Avoid inclement weather.
Do not mix with any solvents.

Do not over thin.  (5% maximum with potable water, to adjust viscosity for environmental conditions.)
Ensure total drying between coats.

Surface must be free of any grease.

Easily thinned with water.

SURFACE PREPARATIONS
For galvanized surfaces, wash with Nyati Ezi Clean or any other galvanized cleaner to ensure total water break free surface.

Use same treatment for steel and other surfaces.  Wire brush, or sand down to provide key into existing painted surfaces, remove all loose or flaking paint, oil, grease, dirt, rust and other deleterious materials.  If required sandblast surface.

Apply Nyati Anti-Corrosive Self-Etch paint to a 140µ WFT minimum.
FIRST AID

Eyes – Wash thoroughly with warm water.  May cause irritation for a few minutes.

SKIN – Not harmful on skin contact.

INGESTION – Not harmful if swallowed in small quantities.  Administer plenty of water.  Do not induce vomiting.

Seek medical attention.
PRODUCT DATA:


RUST INHIBITIVE, SELF ETCH







SEMI – GLOSS, EMULSION PAINT
TECHNICAL DATA

FINENESS OF GRIND:


25 µ maximum
SPREAD RATE:



± 8m² / lt

DRYING TIME:
SURFACE:

1 Hour maximum




HARD:


4 Hours

RECOATING TIME:



1,5 Hours

PH:





4,5 – 10

RESISTANCE TO HEAT:


220 ºC maximum

MIN FILM FORMING TEMP:


3 ºC minimum

VISCOSITY:




80 – 90 KU

SG:





1.33 – 1.37

APPLICATION:

Hydraulic spray equipment.  Brush or roller.
RESISTANCE TO SALF FOG:

250 Hours minimum

CLEANING:
Clean equipment with warm water and soap immediately after use

VOLUME SOLIDS:

45 – 50%

WFT:

70 µ / coat

DFT:

35 µ / coat

APPLICATION TEMP:

10 ºC – 40 ºC

FINISH:

Sheen

ALLOW 48 HOURS TO DRY BEFORE APPLYING AQUANAMEL GLOSS IF REQUIRED
All information is given in good faith, without warranties.  No claim can be made against
NYATI PAINTS since applications, techniques and environmental conditions are beyond our control.

